| Course No. | Course Name | L-T-P-Credits |
| --- | --- | --- |
| CY 538 | Solid State Chemistry | 3-0-0: 03 |
| Prerequisite: NIL |
| Course Objectives: The main objective of the course is to provide an introduction to the concepts underlying solid-state chemistry. The course will be useful for the students to illustrate the wide range of materials and their physical properties that currently available. Course Outcomes: After successful completion of the course, students will be able to: Provide a qualitative description of crystal structures and bonding in solid materials. Define solid-solid phase transition based on thermodynamic, kinetic and structural characteristics of a phase transition and knowledge of some of the most important phase transition in inorganic functional materials Give a qualitative and quantitative representation of 0, 1 and 2-dimensional defects in solids and acquire knowledge of defects related to non-stoichiometry in some important classes of inorganic materials. Understand the structure-property relationship of materials. |
| SYLLABUS |
| Module | Contents | Hours |
| I | Introduction to Crystals and Lattices Unit cells, crystal structure, packing, packing efficiency, coordination number, density of packing in simple cubic, BCC CCP, and HCP structure, tetrahedral, and octahedral holes, radius-ratio, Lattice energy. Structures of Rock salt, zinc blende, Wurtzite, rutile and calcite, perovskite and spinels. | 06 |
| II | Crystal Defects and Non-Stoichiometry Perfect and imperfect crystals, intrinsic and extrinsic defects - point defects, line and plane defects, vacancies - Schottky defects and Frenkel defects, thermodynamics of Schottky and Frenkel defects formation, colour centres, non-stoichiometry and defects. | 04 |
| III | Solid State Synthesis General principles, experimental procedures, high temperature methods, co-precipitation as a precursor to solid state reactions, sol-gel methods, microwave synthesis, high pressure methods for synthesis of solids, kinetics of solid state reactions. | 08 |
| IV | Phase Transformations in Solids Classification and thermodynamics of phase transformations in solids, first order and second order phase transitions, applications of G-T diagrams, kinetics of phase transformations, nucleation and growth mechanism, experimental methods of study of phase transformations. Phase transformation in metals, alloys and compounds. | 04 |
| V | Band Structures of Solids Band structure of metals, insulators and semiconductors, intrinsic and extrinsic semiconductors, doping semiconductors, p-n junctions. | 06 |
| VI | Properties of Solid Optical properties: Optical reflectance, photoconduction - photoelectric effects. Superconductors and electrically conducting solid, organic charge - transfer complex, organic metals, and magnetic properties - classification of materials. Quantum theory of paramagnetics - cooperative phenomenon, magnetic domains, hysteresis, dielectric, ferroelectric and piezoelectric properties of solids. | 08 |

Essential Readings:

1. L. E. Smart and E. A. Moore, “Solid State Chemistry: An Introduction”, CRC Press, 4th Edition, 2012.

2. A. R. West, “Solid State Chemistry and its Applications”, Wiley 2nd Edition, 1999.

Supplementary Readings:

1. C. N. R. Rao, “New Directions in Solid State Chemistry”, Cambridge University Press, 2nd Edition, 1997.